Technical data sheet

ManaFloor EPW-201

Product description:

Two-component water based epoxy Topcoat

Field of application and properties:

ManaFloor EPW-201 is water based epoxy specially designed for floor coatings. Its curing mechanism is done through reaction between two components.

Main characteristics are:

- Odorless

- Easy application

- Water dilutable

- Applicable on wet surface

- Good abrasion resistance

- Water vapor permeable

- Good chemical and mechanical resistance

This type of coating is mainly used for concrete& cement surface, such as: production areas, warehouse, car park decks, garages and etc.

Technical data:

Type: 	Water Borne Epoxy

Color: 	White / Limited colour

Number of components: 	2

Texture: 				Semi -Gloss

Mixing ratio: 	100 / 20

Volume solid: 				62 ±2

Specific gravity: 			1.5 ±0.05

Touch dry at 25° C: 			3 Hrs

Hard dry at 25° C: 			24 Hrs

Fully cured at 25° C: 			7 days

Min over coating time (25° C): 	12 Hrs

Max over coating time: 		48 Hrs

Thinner:                                                   Water

Pot life (20° C): 			60 min

Surface preparation:

Concrete substrates must be prepared by mechanical power tools, weak concrete must be removed and surface defects such as void must be fully exposed and repaired.

The concrete or cement substrate has to be leveled in order to achieve an even surface. Dust, dirt, oil, grease must be completely removed from all surfaces before application of the product.

Method of application:

After surface preparation, first stir the paint component well; note that due to high density of part A, it should be fully mixed to avoid sediment particles, then add part B or hardener to paint in recommended proportion and mix for 3 min. After mixing, use 10-20% water to dilute the mixed component. After that apply coating on the surface by using roller, brush or knife.

STORAGE CONDITIONS:

Store in original sealed containers in a dry and cool warehouse between 10° C and 30° C.